## Slide 1: Activation experiments on neutron beam guide materials
Eszter Dian, Dénes Párkányi, Szabina Török, Péter Zagyvai

## Slide 2: Content
Introduction
Instrumentation
Experiment
Conclusion
Eszter Dian, HAS Centre for Energy Research

## Slide 3: Introduction
Neutron activation
  Radiation protection
  Waste management
Inventory calculation
  Modelling (e.g. NAAPRO)
  Measurement
    Initial composition
    Irradiation
    Spectroscopy
&

## Slide 4: irradiation
Instrumentation

## Slide 5: BRR – Budapest Neutron Centre
VVR-type research reactor
  light water-cooled and moderated tank type reactor with a beryllium reflector
  low enriched uranium fuel (LEU: 19.9% 235U)
nominal thermal power: 10 MW
maximal thermal flux: 2.1 × 1014 n/cm2s
Reactor „campaign”: 10 effective days + break for weekend
~ 160 operational days/year, flexible timetable

## Slide 6
Reactor zone,
vertical irradiation channels

## Slide 7: Irradiation I.
Vertical irradiation channels inside and outside of the zone
  13 irradiation channel
  1 fast neutron channel
  2 B-filtered channel
  …

## Slide 8: Irradiation II.
5 position / channel
  10-10 cm distance
Al capsules as sample holders

## Slide 9: Experiment
Example:
Irradiation of neutron guide

## Slide 10: Neutron Guides
Aluminium samples (1, 2, 3)
Input composition
  Nominal composition
  XRF, µXRF, …
m % |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
No. | V [cm3] | m [g] | Si | Fe | Cu | Mn | Mg | Cr | Ni | Zn | Ti | Zr | Ga | V | Mn | Cr
1 | 1*1*1 | 2.87 | - | - | 2 | - | 2.3 | - | - | 6 | - | - | - | - | - | -
2 | 1*1*1 | 2.72 | 0.4 | 0.4 | 0.1 | 0.4-1.0 | 4.0-4.9 | 0.05-0.25 | - | 0.3 | 0.15 |  |  | - | - | -
3 | 1*1*1 | 2.88 | 0.4 | 0.4 | 0.1 | 0.5 | 2.6-3.6 | 0.3 | - | 0.2 | 0.1 | - | - | - | 0.1-0.6 | 

## Slide 11: Irradiation
Channel 426 (vertical fast neutron channel)
  thermal neutron flux variation along the axis of the irradiation capsule is less than 5 %
  Irradiation time: 6 h
  Cooling time: 6-10 day
Neutron flux parameters | Channel 426 [long-time irradiation]
Thermal neutron flux | 6.00×1013 n cm-2s-1
Fast neutron flux | 5.42×1013 n cm-2s-1

## Slide 12: Irradiation
Vertical irradiation channels inside and outside of the zone
  13 irradiation channel
  1 fast neutron channel
  2 B-filtered channel
  …

## Slide 13: Irradiation
Channel 426 (vertical fast neutron channel)
  thermal neutron flux variation along the axis of the irradiation capsule is less than 5 %
  Irradiation time: 6 h
  Cooling time: 6-10 day
Neutron flux parameters | Channel 426 [long-time irradiation]
Thermal neutron flux | 6.00×1013 n cm-2s-1
Fast neutron flux | 5.42×1013 n cm-2s-1

## Slide 14: γ-spectroscopy
3 low-level chambers
  pre-World War II steel
    free of any man-made radioactivity
    10 cm thick wall
    2 mm thick Cu-lining (attenuate the X-rays)
  HPGe detectors
Detectors | Efficiency | Resolution [59.5 keV] | Resolution [1332.5 keV]
ORTEC PopTop 55195-P HPGe detector | 55% | 0.95 keV | 1.75 keV
Canberra GC3618 HPGe detector | 36% | 0.80 keV | 1.80 keV
Canberra GC1318 HPGe detector | 13% | 0.95 keV | 1.80 keV

## Slide 15: Results I. - NA
Zn-65
E=1115.54 keV
T1/2=244.3 d
Cr-51
E=320.08 keV
T1/2=27.7 d
Isotope | A (Bq) |  | 
 | 1 | 2 | 3
Zn-65 | 5.20E+07 | 5.93E+04 | 4.98E+07
Cu-64 | 3.81E+06 | - | 4.02E+06
Na-24 | 5.52E+05 | 6.51E+05 | 5.19E+05
Ga-72 | 4.38E+04 | 3.15E+04 | -
Mn-54 | 4.67E+04 | 3.41E+04 | -
Fe-59 | 4.59E+04 | 4.83E+04 | 4.78E+04
Co-60 | - | 8.47E+03 | 1.21E+04
Sc-46 | - | 7.19E+03 | -
Co-58 | - | 9.93E+03 | -
Cr-51 | - | 3.95E+06 | 3.09E+06
Zr-95 | - | - | 7.07E+04

## Slide 16: Results II. - XRF
m % |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
No |  | V [cm3] | m [g] | Si | Fe | Cu | Mn | Mg | Cr | Ni | Zn | Ti | Zr | Ga | V
1 | Nom | 1*1*1 | 2.87 | - | - | 2 | - | 2.3 | - | - | 6 | - | - | - | -
 | XRF |  |  | - | 0.18 | 2.38 | 0.03 | - | 0.07 | - | 8.63 | - | 0.03 | 0.02 | -
2 | Nom | 1*1*1 | 2.72 | 0.4 | 0.4 | 0.1 | 0.4-1.0 | 4.0-4.9 | 0.05-0.25 | - | 0.3 | 0.15 |  | - | -
 | XRF |  |  | - | 0.33 | 0.03 | 0.64 | - | 0.09 | 0,01 | 0.02 | - | - | 0.01 | 
3 | Nom | 1*1*1 | 2.88 | 0.4 | 0.4 | 0.1 | 0.5 | 2.6-3.6 | 0.3 | - | 0.2 | 0.1 | - | - | -
 | XRF |  |  | - | 0.2 | 2.4 | 0.01 | - | 0,.3 | - | 8.98 | - | 0.03 | 0.00 | -

## Slide 17: Results III.
Isotope | A (Bq) |  |  |  |  | 
 | Al sample 1 |  | Al sample 2 |  | Al sample 3 | 
 | Meas. | Calc. | Meas. | Calc. | Meas. | Calc.
Zn-65 | 5.20E+07 | 3.35E+07 | 5.93E+04 | 5.69E+04 | 4.98E+07 | 3.50E+07
Cu-64 | 3.81E+06 | 3.39E+06 | - | 2.46E+04 | 4.02E+06 | 3.37E+06
Ga-72 | 4.38E+04 | 3.40E+04 | 3.15E+04 | 1.66E+04 | - | 3.06E+03
Mn-54 | 4.67E+04 | 7.42E+03 | 3.41E+04 | 1.40E+04 | - | 8.74E+03
Fe-59 | 4.59E+04 | 4.13E+04 | 4.83E+04 | 4.88E+04 | 4.78E+04 | 4.89E+04
Co-60 | - | - | 8.47E+03 | 1.22E+04 | 1.21E+04 | 3.92E+03
Co-58 | - | - | 9.93E+03 | 1.38E+04 | - | -
Cr-51 | - | - | 3.95E+06 | 3.72E+06 | 3.09E+06 | 2.03E+06

## Slide 18: Conclusion I.
Activation products:
  Radiation protection
  Waste management
Nominal composition is not always reflecting the real elemental chemistry
Zn-65
  T1/2=244.3 d
Cr-51
  T1/2=27.7 d
Aluminium sample No. 2

## Slide 19: Conclusion II.
Know-how
  considerable experience in
    neutron activation
    material testing methods
    γ-spectroscopy
Facilities
  various irradiation channels & fluxes
  analytical devices

## Slide 20: Thank you for your attention!